## Slide 1: Slac Trip B Sample Information Sheet
Created: 1.21.2017

## Slide 2: Informational Sheets
These sheets list the ternary map and the compositional diagram. On each compositional diagram, the flat is on the left. The element of each composition diagram is listed next to its corresponding color bar.
All samples have their index number scribed on the back center of the sample, and a Roman numeral 2 directly under the flat, to indicate that they are the second (B) batch of samples.
Composition predictions were made using an in-house sputtering prediction model

## Slide 3: B1 MG-12/2/16-TMW-01 Co-Cr-Zr

## Slide 4: B2 MG-12/2/16-TMW-02 Co-Cr-Zr

## Slide 5: B3 MG-12/2/16-TMW-01 Co-Cr-Zr

## Slide 6: B4 MG-12/8/16-TMW-01 Co-Ti-Zr

## Slide 7: B5 MG-12/12/16-TMW-01 Co-Ti-Zr

## Slide 8: B6 MG-12/13/16-TMW-01 Co-Ti-Zr

## Slide 9: B7 MG-12/16/16-TMW-01 Cr-Ti-Zr

## Slide 10: B8 MG-12/16/16-TMW-02 Cr-Ti-Zr

## Slide 11: B9 MG-12/19/16-TMW-01 Cr-Ti-Zr

## Slide 12: B10 MG-12/19/16-TMW-02 Co-Cr-Ni

## Slide 13: B11 MG-12/20/16-TMW-01 Co-Cr-Ni

## Slide 14: B12 MG-12/20/16-TMW-02 Co-Cr-Ni

## Slide 15: B13 MG-1/6/17-TMW-01 Ni-Si-Ti

## Slide 16: B14 MG-1/6/17-TMW-02 Ni-Si-Ti

## Slide 17: B15 MG-1/9/17-TMW-01 Ni-Si-Ti

## Slide 18: B16 MG-1/9/17-TMW-02 Ni-Nb-Ti

## Slide 19: B17 MG-1/10/17-TMW-01 Ni-Nb-Ti

## Slide 20: B18 MG-1/10/17-TMW-02 Ni-Nb-Ti

## Slide 21: B19 MG-1/11/17-TMW-01 Fe-Nb-Ti

## Slide 22: B20 MG-1/11/17-TMW-02 Fe-Nb-Ti

## Slide 23: B21 MG-1/12/17-TMW-01 Fe-Nb-Ti

## Slide 24: B22 MG-8/22/16-TMW-01 Co-Fe-V

## Slide 25: B23 MG-8/22/16-TMW-02 Co-Fe-V

## Slide 26: B24 MG-8/26/16-TMW-01 Co-Fe-V